| SECTION 07430 - EXTERIOR WOOD COMPOSITE PANELS PARKLEX FACADE * NOTE TO SPECIFIER: Manufactured by: Composites Gurea, S.A. Zalain Auzoa 13 31780 Vera de Bidasoa, Navarra Spain http://www.parklex.com/ PART 1 - GENERAL 1.1 WORK A. Provide everything required to complete the work as shown on the Drawings and specified herein. 1.2 QUALITY STANDARDS A. Provide experienced, well-trained workers competent to complete the work as specified. Fabricator/installer shall be experienced in performing work of similar type and scope. B. Unless approved by the Architect, provide all related products and accessories from one manufacturer. C. Ventilated rainscreen system shall provide complete secondary drainage system, draining at base of wall. Supporting substrate for exterior wall panels shall comply with all current codes and regulations. 1.3 SUBMITTALS A. Submit the following within 30 calendar days after receiving the Notice to Proceed. *Note to specifier: Submittals are usually required within a specified number of calendar days after the Contractor is given the Notice to Proceed. 30 calendar days is a common requirement for medium- to large-size projects. Your choice of time will depend on the size of the project and the Owner's need for an expedited schedule. B. Submit list of materials to be provided for this work; manufacturer's data required to prove compliance with these Specifications, manufacturer's installation instructions; shop drawings of the ventilated rainscreen system, as required, with complete details and assembly instructions. C. Submit samples as required for approval by the Architect. *Note to specifier: Samples may be requested with a different time limit than other submittals. Details of the samples requested -- sizes, finishes, etc. -- are usually specified. Delete selection samples if colors have already been selected. D. Shop Drawings for Ventilated Rainscreen System: Shop Drawings shall be complete with specific instructions for the installation of panels, sub-frame assemblies and other component parts. Include engineering analysis. Drawings shall indicate sizes of ventilation openings and methods of preventing unwanted insects or animals from entering cavity behind panels. 1.4 PRECONSTRUCTION AND PREPARATION A. Examine and verify that job conditions are satisfactory for speedy and acceptable work. B. Field Measurements: Secure field measurements before preparation of shop drawings and fabrication where possible, for proper fabrication and installation of the work. C. Pre-installation Meeting: Conduct pre-installation meeting to verify project requirements, substrate conditions, manufacturer's installation instructions and manufacturer's warranty requirements. 1.5 DELIVERY, STORAGE, AND HANDLING A. Deliver materials in manufacturer's original, unopened, undamaged containers with identification labels intact. Materials must be transported flat and kept dry and protected from the elements and handled with care. B. Storage and Protection: Materials must be stored flat and kept dry in a warehouse/storage facility, protected from exposure to harmful weather conditions, at temperatures and humidity conditions recommended by the manufacturer. 1.6 PROJECT CONDITIONS A. Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's absolute limits. 1.7 WARRANTY A. Project Warranty: Refer to Conditions of the Contract for project warranty provisions. B. Manufacturer's Warranty: Submit, for Owner's acceptance, manufacturer's standard warranty document executed by authorized company official. Manufacturer's warranty is in addition to, and not a limitation of, other rights Owner may have under Contract Documents. PART 2 PRODUCTS 2.1 MANUFACTURERS A. Provide PARKLEX FACADE [Exterior Grade Wood Composite Panels] Local Representative Contact: Pacific Sales Group Northwest - Todd Johnson 360-451-1130 tjohnson@pacificsalesgroupnw.com Manufactured by: Composites Gurea, S.A. Zalain Auzoa 13 31780 Vera de Bidasoa, Navarra Spain http://www.parklex.com/ B. Substitutions: Not Permitted. 2.2 MATERIALS A. EXTERIOR GRADE WOOD COMPOSITE PANEL: High-density stratified timber panel manufactured from kraft paper treated with resins thermoset under high pressure and temperature, finished with natural timber veneers highly resistant to UV radiation and atmospheric agents. B. Decorative paper simulating wood veneer is not acceptable. 1. WOOD VENEER: GOLD AMBAR RUBI COPPER ONIX ANTRA QUARTZ SILVER Smooth surface (standard). * NOTE TO SPECIFIER: Delete veneers not used on the project. 2. PANEL DIMENSIONS: 1220mm (48") x 2440mm (96") x thickness. Thickness: 8mm, 10mm, 12mm * NOTE TO SPECIFIER: Delete thicknesses not used on the project. 3. DIMENSIONAL TOLERANCES: Length ±2mm, Width ±2mm, Thickness ±0.55mm (10mm thick panel). 4. WEIGHT: (8mm); 1220mm x 2440mm x 8mm panel weighs approximately 73 pounds. (10mm); 1220mm x 2440mm x 10mm panel weighs approximately 93 pounds. * NOTE TO SPECIFIER: Delete thicknesses not used on the project. 5. SURFACE BURNING CHARACTERISTICS: Report on surface burning characteristics determined by ASTM E-84 (twenty-five foot tunnel furnace test method)Standard (S) panel, meets Class B (II) - 75 or under flame spread, with a flame spread index of 40 and smoke developed index of 35. Class A (Class I) rating - with a flame spread index of 5 and smoke developed index of 10 is available in (F) panel. 6. Resistance to UV Light: EN438-2:2005 apt. 29. Panels must be tested for minimum or 3000 hours of exposure to Xenon Arc lamp resulting in a minimum grey scale rating of 3 and an appearance grade of 5. 7. THERMAL PROPERTIES: Parameter Description Metric English Thermal Conductivity k 0.18 W/m·K 0.104 (Btu/h)/ft·F Thermal Resistance R (10mm) 0.0556 K·m2/W 0.315 h·ft2·F/Btu Equivalent to R-9.61 (thermal resistance of 1 ft of Parklex insulation, given in h·ft2·F/Btu). 8. TECHNICAL DATA: ASTM Test Results Characteristics Standards and test methods Values Density (10mm) ASTM D 2395 Method A 1.51 g/cc Moisture Content ASTM D 4442 Method A 2.1% Water Absorption (24 h/23°C) ASTM D 1037 Method B 0.34% by mass 0.56% by volume Thickness Swelling 0.59% Flexural Properties ASTM D 1037 Modulus of Elasticity veneer parallel to long dimension dry soaked 19.0 GPa (2,756,000 psi) 18.0 GPa (2,611,000 psi) veneer perpendicular to long dim. dry soaked 9.0 GPa (1,305,000 psi) 8.7 GPa (1,261,000 psi) Bending Strength (MOR) parallel to long direction dry soaked 193 MPa (28,000 psi) 200 MPa (29,000 psi) perpendicular to long direction dry soaked 93 MPa (13,500 psi) 108 MPa (15,700 psi) Bond Durability APA PS-1 6.1.5 maximum load reference vacuum/pressure soaked boiled (2 cycles) 2.58 kN (580 lb-f) 3.47 kN (780 lb-f) 2.68 kN (600 lb-f) Surface Burning Characteristics ASTM E-84 Class B (II) / Class A (I) 9. EUROPEAN TEST RESULTS: Characteristics Standards and test methods Values Visible Density UNE 53.020 (NF T 51-005) 1.4 gr/cc (> 1400 daN/m3 ±50) Water Absorption 24 h/23°C <1.5% in mass Moisture Content --- <1% Formaldehyde Content UNE-EN 312-1:1.997 Class 1 (<1 mg/100g) (9 ppm - parts per million) Bending Strength lengthways crosswise ISO 178 190 MPa 95 MPa Stretch Modulus lengthways crosswise ISO 178 >18,000 MPa >7,800 MPa Traction Shearing NF EN 314-1 1) 2x4 h in boiling water 2) 72 h in boiling water ShearingR N/mm2/80% adhesion ShearingR N/mm2/70% adhesion Compression Strength ISO 604 220 MPa External Glueing Quality EN 311 72 h boiling water surface tearing <4MPa Toughness UNE 56.534/77 16.8 Resistance to Abrasion UNE 23-727/90 (EN 438) 1,200/13,000 cycles (7,000) Resistance to Stains EN 438 5 Resistance to Cigarette Burns EN 438 2 Fire Reaction UNE 23-727/90 Class M2/M1 Fume Toxicity/Opacity --- Class F1 2.3 FABRICATION A. Fabricate composite panels and accessory items in accordance with manufacturer's recommendations and approved submittals. B. Fabricate panels to sizes indicated. PART 3 EXECUTION 3.1 INSPECTION A. Examine alignment of backup structure prior to installing sub-frame. Do not proceed until all defects are corrected. 3.2 INSTALLATION A. Comply with Manufacturer’s “General Guidelines for Panel Installation” available at http://www.parklex.com B. Attachment System: Concealed fixing system as per manufactures system details. Vertical supports allowing 1” minimum cavity behind panels to allow sufficient air flow. C. Install solid exterior wall panels plumb and level and accurately spaced in accordance with manufacturer's recommendations and approved submittals. D. Fasten solid exterior wall panels to supporting substrate with fasteners approved for use with adjoining construction. E. Interface with Other Work: * NOTE TO SPECIFIER: Include adjacent surfaces to which panels must adjoin. 1. [Specify applicable requirements for interface with other work.]. F. Accessory Items: Install corner profiles, gaskets and trim [Insert accessory items.] with fasteners and adhesive appropriate for use with adjoining construction as indicated on drawings and as recommended by manufacturer. 3.3 DAMAGED MATERIAL A. Repair or replace all damaged material to the satisfaction of the Architect. 3.4 CLEANING A. Do not use abrasive cleaners or cleaning tools. Dry wipe down panel sections as work progresses. B. Provide final cleaning of the wall system. 3.5 PROTECTION A. Protect installed product and finish surfaces from damage during construction. END OF SECTION |  |
| --- | --- |